
     Ningbo GLD Packing&Gasket Co.,Ltd. 
[image: image1.jpg]


DATA SHEET
[image: image2.jpg]AR D A B D BDA ASD S
I LA S P I
D e B Bt o o
Bl et o ot g et o b

DA B D "9«va¢
e P o D ﬁ




White PTFE Packing
GLD- 150, 150L                                    

PTFE has characteristics of excellent anticorrosion, good self-lubrication and non-sticking. However, it is also substance with low heat conductivity, cold flow and great thermal expansion coefficient. All of GLD PTFE packings are designed for every applications.

CONSTRUCTION:

150(A/B) Pure PTFE Packing (Free oil)

Braided from pure PTFE yarn without any lubrication. It is soft, mainly for static sealing. 

150P=150 + PTFE Impregnation
150L(A/B) Pure PTFE Packing with oil

Same as 150, but treated with special lubrication, designed for dynamic.

GLD 150 & 150L both are economical packing.
APPLICATION:


	150(A/B)
	Designed for valves and lower shaft speed applications under medial pressure in food processing, pharmaceuticals, paper mills, fibre plants where high purity and corrosion resistance is required.

	150L
	Universal, suitable for valves, pumps and agitators in most mediums.


PARAMETER:
	Style
	150(A/B)
	150L(A/B)

	Pressure
	Rotating
	15 bar
	15 bar

	
	Reciprocating
	100 bar
	100 bar

	
	Static
	150 bar
	200 bar

	Shaft speed
	2 m/s
	10m/s

	Density
	1.3g/cm3
	1.6 g/cm3

	Temperature
	－150~+260°C

	PH range 
	0~14


ACKAGING:
in coils of 5 to 10 kg, other weight on request;  
as precut length; 
as packing rings----R150,R150L

DIMENSIONS:

	Size mm
	4
	5
	6
	8
	10
	12
	14
	15
	16
	18
	19
	20

	appr. m/kg
	35
	22
	16
	9.0
	5.6
	3.9
	2.9
	2.5
	2.2
	1.7
	1.5
	1.4

	Appr. ft/lb
	52
	33
	24
	14
	8.3
	5.8
	4.3
	3.7
	3.3
	2.5
	2.9
	2.1

	kg/coil
	5 or 10


Above appr. Weight for type 150L









All data quoted are based on our extensive tests and years of experience, however, they can only serve as guide values. Failure to select proper sealing products could result in property damage and/or serious injury. Specifications are subject to change without notice.                                                              

